DETECNICKS

LTD.

3 Orchard Crescent, Arundel Road, Fontwell

West Sussex BN18 0SD

Tel:01243 545060 Fax: 01243 545922

Internet: HTTP://www.detecnicks.co.uk

e-mail; sales@detecnicks.co.uk

VAT reg. no 712132978					Reg. Co. No.3737696

E.D.T.A.

(Ethylene-diamine-tetra-acetic Acid)

Used as a corrosion remover on copper alloys, lead and tin alloys and pewter.

The container contains sufficient e E.D.T.A. to make a 5% solution in half a litre of water. The mixed solution usually remains active for approximately 2 years.

Prior to application, remove oil, grease & dirt and any superficial corrosion from the object. The item should then be fully submersed in the mixed solution and left until the white oxide coating in the case of lead & tin alloys has dissolved

Iron corrosion on copper alloys can be dissolved using the same process.

IT IS NECESSARY TO MONITOR THE PROCESS AS PROLONGED TREATMENT CAN RESULT IN THE ITEM BEING STRIPPED BACK TO THE BARE METAL.

After removal from the solution wash thoroughly under running water.

E.D.T.A. solution should be discarded when it becomes cloudy.

E.D.T.A. solution should be used with care. Ensure the solution does not come into contact with the eyes or skin. Rinse contaminated parts well with running water and seek medical advice.

Lead is poisonous and should not be inhaled or ingested.

All spillages should be cleaned up straight away.

Wear protective gloves, and use in a well-ventilated place.

Dispose of used solution in a safe and suitable place.

The above instructions on cleaning are intended as a guide and we cannot guarantee results of the cleaning process.

________________________________________________________

Registered Office:

24 North Way, Felpham, West Sussex, PO22 7BT

Director: N. Charman.